Strata 30 DryShot

30 MPa Factory Pre-Blended Dry-Mix Shotcrete

P R O D U C T   D A T A   S H E E T

| Document reference | SAAM-S30DS-PDS-001 |
| --- | --- |
| Issue | Issue 1, 2026 |
| Manufacturer | Shotcrete Africa Advanced Materials |
| Application class | Underground mining · Tunneling · Ground support |

Chemistry · Science · Performance

# 1  GENERAL DESCRIPTION

Strata 30 DryShot is a ready-to-use, factory pre-blended dry-mix shotcrete (gunite) formulation engineered for underground mining, tunneling, and ground support applications. It is designed to achieve a minimum compressive strength of 30 MPa at 28 days under SANS 5863.

The formulation incorporates a precisely graded aggregate blend, OPC and pozzolanic binder components to deliver consistent adhesion, minimised rebound, and reliable application performance in confined or damp underground conditions.

TRUE PRE-BLEND TECHNOLOGY

Break the bag. Load the hopper. Shoot. Strata products are factory pre-blended to a single homogeneous mix. The bag breaks directly into the gunite pot or rig hopper — no site mixing, no pan mixer, no inner bag, no guesswork. Key advantages: - Factory-controlled homogeneous blend — same ratio, same performance, every bag - No pan mixer required underground — eliminates equipment, space, and maintenance in confined headings - No hand mixing on the floor — eliminates a labour step and the inconsistency that comes with it - Faster cycle times — bag in, shoot, move on - Reduced contamination risk — no open mixing on a mine floor

Typical applications:

- Primary and secondary ground support in underground mining

- Lining of tunnels, shafts, and crosscuts

- Construction of ventilation walls, seals, and bulkheads

- Rock stabilisation on excavated slopes and portals

- Concrete rehabilitation and spall repair in underground facilities

# 2  SPECIFICATIONS

2.1  Binder system

| OPC (CEM I 52.5N) | Primary binder |
| --- | --- |
| Pozzolanic agents (fly ash / silica fume) | Secondary binder — enhances adhesion and reduces permeability |

2.2  Mechanical performance

| Compressive strength @ 24 hours | 3 MPa (SANS 5863) |
| --- | --- |
| Compressive strength @ 7 days | 18 MPa (SANS 5863) |
| Compressive strength @ 28 days | 30 MPa minimum (SANS 5863) |
| Adhesion to rock substrate | Good — suitable for direct application to clean damp rock |
| Rebound | Low — proprietary aggregate grading minimises waste |

2.3  Physical and application properties

| Application method | Dry-mix shotcrete (gunite) — bag directly into hopper, no site mixing |
| --- | --- |
| Recommended nozzle pressure | 8 bar |
| Recommended applied thickness | +50 mm per layer; 100 mm layers achievable |
| Pot life | 90 minutes after air/moisture exposure |
| Dry density | ~1.40 kg/L |
| Wet density | ~2.20 kg/L |
| Pack size | 30 kg bags (standard). 1 000 kg bulk bags available. |
| Yield per 30 kg bag | Approximately 15 L of placed shotcrete |
| Yield per 1 000 kg bulk bag | Approximately 495 L of placed shotcrete |
| Coverage | Approximately 67 × 30 kg bags per m³ placed (based on 180 L/m³ water addition, wet density 2 200 kg/m³) |
| Colour | Grey |
| Shelf life | 12 months from manufacture in original sealed packaging, dry cool storage |

# 3  OPTIONAL ENHANCEMENTS

3.1  Macro-Synthetic Fibres (40 mm)

- Increased energy absorption (toughness) and impact resistance

- Reduced shrinkage-related cracking

- Safer in man-ways and personnel contact areas than steel fibres

- Improved adhesive and cohesive plastic properties

3.2  Accelerator additives

- Enables faster re-entry and improved production cycle times

- Tailorable to ambient temperature and project requirements

Note: Contact Shotcrete Africa Advanced Materials for approved accelerator specifications and dosage guidance.

# 4  PACKAGING AND SHELF LIFE

- Supplied in 30 kg paper bags, palletised under shrink wrap. 1 000 kg bulk bags available on request.

- Shelf life: 12 months from manufacture in original sealed packaging in dry, cool conditions off the ground

- Each batch supplied with batch number, manufacture date, and mix verification documentation

# 5  STORAGE

- Store dry — product must not be exposed to rain, condensation, or high humidity

- Store off the ground on pallets

- Rotate stock on a first-in, first-out basis

# 6  GUIDELINES FOR APPLICATION

6.1  Substrate preparation

- Remove all loose, delaminated, deteriorated or contaminated material to expose a sound substrate

- Remove all loose rock by mechanical scaling

- Saturate substrate to SSD condition immediately before application; no standing water

- Ensure surface temperature is at or above +10 °C prior to application

6.2  Loading and application

- Break the bag directly into the gunite pot or rig hopper — no site mixing required

- Apply clean potable water at 8 bar nozzle pressure

- Ensure substrate is damp, clean, and free of loose material before application

- Apply in layers to achieve design thickness

- Application to be carried out by ACI Certified Nozzlemen

6.3  Curing

- Acrylic curing compounds recommended — wax-based not suitable if additional layers are to follow

- Fogging to 100% humidity preferable where conditions allow

- Protect from direct sun and wind during initial curing period

# 7  LIMITATIONS

- Not for use at substrate or ambient temperatures below +5 °C or above +35 °C without modified procedures

- Application by a competent and trained shotcrete nozzleman, in accordance with ACI 506R guidelines

- Do not mix with other cementitious systems in equipment without thorough cleaning

# 8  HEALTH AND SAFETY

Strata 30 DryShot is a cementitious product. Refer to the Strata 30 DryShot Safety Data Sheet (SDS) before handling, storage, mixing or application. Approved personal protective equipment shall be worn at all times, including P2/FFP2 dust mask or respirator, eye protection, alkali-resistant gloves, and overalls. In the event of skin or eye contact, flush thoroughly with clean water and seek medical attention if irritation persists.

# 9  MANUFACTURER AND TECHNICAL CONTACT

| Manufacturer | Shotcrete Africa Advanced Materials Chemistry · Science · Performance CT Office: 021 180 5480 · JHB Office: 011 027 4227 · Mobile: +27 79 495 4337 dustin@shotcrete.co.za www.shotcrete.co.za/advancedmaterials |
| --- | --- |
| Technical consultant | Jaco du Plessis (B.Eng Civil) Concrete Technologist, Go Consult Tel: 082 554 3694 |

Disclaimer

Shotcrete Africa Advanced Materials warrants that the product conforms to the specifications stated in this data sheet at the point of supply. No representation or warranty of fitness for any particular purpose is given, either express or implied. Technical advice and information are provided in good faith based on current knowledge and experience. The user is responsible for verifying that the product is appropriate for the intended application. Liability for any non-conforming product is limited to product replacement or refund of purchase price at the manufacturer's option.

Strata and Shotcrete Africa Advanced Materials are trademarks of Shotcrete Africa.